Applied Technologies, LLC

P. O. Box 18476

Fairfield, OH  45018

1-877-277-5948

(513) 939-3767

Section 33 46 16.16 (MF 04)

(Formerly 2621 MF 95)

Geocomposite Foundation Drainage

This specification utilizes the Construction Specifications Institute (CSI) Manual of Practice, including MasterFormat and PageFormat.  This is a manufacturer-specific proprietary product specification using the proprietary method of specifying applicable to project specifications and master guide specifications.  Optional text is indicated by bracket [] delete optional text in final copy of specification.  Specifier notes typically precede specifications text; delete notes in final copy of text specification.  Trade/brand names with appropriate symbols typically are used in Specifier Notes; symbols are not used in specification text.  Metric conversion, where used is soft metric conversion.

The specification specifies DrainGuard Geocomposite Drainage.  This product is manufactured by Applied Technologies LLC. Revise section number and title to suit project requirements, specification practices and section content.  Refer to CSI MasterFormat for other section numbers and titles.

# Part 1 General

  - SUMARRY

- Section Includes: DrainGuard subdrainage system material at vertical **waterproofed walls** lagging ** as complete designed working drainage system channeling liquid water to **

  - **drainage piping system specified elsewhere

  - ** Modular Chimney Drainage system specified in this Section; connection to piping system specified elsewhere

  - **Vertical Collection System specified in this section; connection to piping system specified elsewhere.

Specifier Note: Article below may be omitted when specifying manufacturer’s proprietary products and recommended installation.  Retain Reference Article when specifying products and installation by an industry reference standard.  If retained, list standard reference in this section.  Indicate issuing authority name, acronym, standard designation and title.  Establish policy for indication edition date of standard referenced.  Conditions of the Contract or Division 1 References Section may establish the edition date of standards.  This article does not require compliance with standard, but is merely a listing of references used.  Article below should list only those industry standards referenced in this section.

Specifier Note: Use 06 10 00 If wood strips are used.

Specifier Note: Delete 01 25 13 if no substitutions are allowed or you have coordinated front end documents that need no actual reference to Division 01

- Related Sections:

  - Section 012513-Product Substitution Procedures

  - Section 033000-Cast in Place Concrete

  - Section 061000-Rough Carpentry

  - Section 071210 Waterproofing

  - Section 071300-Membrane Waterproofing

  - Section 071400-Cold Fluid Applied Waterproofing

  - Section 071700-Bentonite Waterproofing

  - Section 312000-Earth Moving

  - Section 312310-Building Excavation and Fill

  - REFERENCES

- American Society for Testing and Materials (ASTM)

  - DEFINITIONS

A. 	Terms; 1 through 4 taken from ASTM D4439

1. 	Geotextile-Any Permeable textile used with foundation, soil, rock, earth or any 					other geotechnical material, as an integral part of man-made product, structure, 					or system.

2. 	Normal Direction-Direction perpendicular to the plane of a geotextile

3. 	Permittivity-Volumetric flow rate of water per unit cross sectional area per unit 					head under laminar flow conditions, in the normal direction through a 						geotextile.

4. 	Permeability-Rate of flow of a liquid under a differential pressure through a 						material.

5.	Transmissivity-Flow or amount of liquid water per foot of material width passing 					through composite system at certain maximum soil pressure against geotextile 					at defined hydraulic gradient

1.04   SYSTEM DESCRIPTION

Specifier Note: UV resistance requirements necessary to allow backfill or cover material is in place 60 days maximum from installation, although not immediately required if weather and construction sequencing do not permit.

A. 	Performance Requirements:

1. 	Geotextile:

a.	UV Resistance: 70% or more when tested in accord with ASTM D-4355-					02.

b. 	Permittivity: 150 gal/min/ft2 (6105 l/min/m2) when tested in accord with 							ASTM D-4491-99a.

2.	Core Material, Compressive Strength: Specified in PART 2-Products Article 						below for selected materials.

3. 	Transmissivity or Flow Q with hydraulic gradient of 1 with confining stress 						indicated in MANUFACTURED UNITS Article in accord with ASTM D-4716-01.

1.05 SUBMITTALS

A. 	Product Data: Manufacturer's product data; indicate products supplied.  Provide 					complete installation instructions proposed for use.

B. 	Samples:

1.  Subdrainage system material: 3"x3"

**2. Modular chimney drainage system material: 4" length

**3. Vertical collection drainage system material: 4" length

1.06 QUALITY ASSURANCE

- Applicator Qualifications: Utilize an applicator trained and approved by waterproofing manufacturer.

- Preinstallation conference: Coordinate with conference scheduled for waterproofing materials. Follow requirements indicated in waterproofing materials section.

1.07 DELIVERY, STORAGE AND HANDLING

A.	General; Comply with Division 1 Product Requirement Section

B. 	Delivery: Deliver materials in manufacturer’s original, unopened, undamaged 						containers with identification labels intact.

1.08 SEQUENCING AND SCHEDULING

A. Schedule installation after waterproofing has been installed and before backfilling.

1.09 Warranty

A. 	Material Warranty: Applied Technologies (Applied) warrants that materials and products are free 	of 			manufacturing defects at the time of manufacture.  If any Applied materials prove to contain manufacturing 		defects that substantially effect their performance, Applied, will at its option replace the materials or refund the 		purchase price of the materials in question.

This limited warranty is the only warranty extended by Applied.  There are no other warranties including the 	implied warranty of merchantability and fitness for a particular purpose.  Applied specifically disclaims liability 	for any incidental, consequential or other damages or including but not limited to loss of profits or damages to a 	structure or its contents arising under any theory whatsoever.

The dollar value of Applied's liability and buyer's remedy under this limited warranty shall not exceed the 	purchase price of the Applied material in question.

PART 2- PRODUCTS

2.01 Manufacturer

A. Products in this section manufactured by Applied Technologies, LLC

1. Contact: P. O. Box 18476 Fairfield, OH 45018 1-877-277-5948 (513) 939-3767 				Fax (513) 939-3787

B. Dimple Core Drainage Material

1. Type **

** DrainGuard 400; heavy duty core, single sided fabric

** DrainGuard 420; heavy duty core, single sided fabric, protective sheet on dimple 					 core backside

** DrainGuard 700; heavy duty core, single sided fabric

** DrainGuard 720; heavy duty core, single sided fabric, protective sheet on dimple 					 core backside

2. Core:

a. Material: High impact polypropylene

b. Type: formed dimple core

c. Compressive strength:

** DrainGuard 400/420: 15,000 PSF (719 kN/m2)

** DrainGuard 700/720: 21,000 PSF (1005 kN/m2)

3. Geotextile **

a. ** DrainGuard 400/420

i.   Material: Non-woven needle punch polypropylene

ii.  Weight: 4.0 oz per sq. yard (136 g/m2), minimum

iii. Treat fabric to meet UV requirements as outlined in SYSTEM 						   	    	 DESCRIPTION above.

iv. Permittivity: Meet requirements in SYSTEM 						   		     	      DESCRIPTION above.

b. ** DrainGuard 700/720

i.   Material: Woven monofilament polypropylene

ii.  Weight: 5.6 oz per sq. yard (190 g/m2), minimum

iii. Treat fabric to meet UV requirements as outlined in SYSTEM 						        		   DESCRIPTION above.

iv. Permittivity: Meet requirements in SYSTEM 						   		       		    DESCRIPTION above.

4. Adhesive bonding core material to geotextile: Pressure sensitive applied to core, 				   	 manufacturer's standard

Specifier Note: Select same series as specified above for Flow Q.

5. Transmissivity or Flow Q of composite construction, geotextile bonded to core 							when tested in accord with ASTM D-4716-01 with hydraulic gradient of 1 with 							confining stress of 3600 PSF: **

a. DrainGuard 400: 18.0 gallons/min/ft (223 lpm/m)

b. DrainGuard 700: 21.0 gallons/min/ft (261 lpm/m)

Specifier Note: DrainGuard 6" or 12" chimney drainage system specified in this section is an economical wall drainage system.  Chimneys are placed 4' to 6' on center

Specifier Note: DrainGuard 6" can substitute pipe and gravel collection system

Specifier Note: End outlet and side outlet for transition to 4" pipe collection system as specified in another section are available.

Specifier Note: Use deeper than 30' requires consultation with Applied Technologies prior to installation

C. Modular Chimney Drainage System Material

1. Type: DrainGuard 6" Modular Drainage System

2. Size" 6" high x 1" thickness x 150' roll

3. Core:

a. Material: High impact polystyrene

b. Type: Formed dimpled core

c. Compressive strength: 9,500 PSF (455 kN/m2)

4. Geotextile:

a. Material: Non-woven needle punch polypropylene

b. Weight: 4.0 oz per sq. yard (136 g/m2), minimum

c. Treat fabric to meet UV requirements as outlined in SYSTEM 						   	     DESCRIPTION above.

d. Permittivity: Meet requirements in SYSTEM DESCRIPTION above.

5. Adhesive bonding core material to geotextile: Pressure sensitive applied to core, 						 manufacturer's standard.

6. Transmissivity or Flow Q of composite construction, geotextile bonded to core 					when tested in accord with ASTM D-4716-01 with hydraulic gradient of .1 with 					confining stress of 3600 PSF: 30.0 gallons/min/ft (372 lpm/m)

7. Furnish manufacturer's 6"x6" corner fittings and 6"x 4" end outlet, 6"x 4" side 			 		outlet and 6" x 4" corner outlet fittings with 4" diameter female connector for  connection to 4" 			diameter corrugated plastic piping system specified elsewhere.

Specifier Note: Vertical collection system can be used to replace pipe and stone collection system when used in conjunction with DrainGuard 400/420/700/720

Specifier Note: End outlet and side outlet for transition to 4" pipe collection system as specified in another section are available.

D. Vertical Collection Drainage System

1. Type: DrainGuard 12" Vertical Collection System

2. Size" 12" high x 1" thickness x 150' roll

3. Core:

a. Material: High impact polystyrene

b. Type: Formed dimpled core

c. Compressive strength: 9,500 PSF (455 kN/m2)

4. Geotextile:

a. Material: Non-woven needle punch polypropylene

b. Weight: 4.0 oz per sq. yard (136 g/m2), minimum

c. Treat fabric to meet UV requirements as outlined in SYSTEM 						   	     DESCRIPTION above.

d. Permittivity: Meet requirements in SYSTEM DESCRIPTION above.

5. Adhesive bonding core material to geotextile: Pressure sensitive applied to core, 						 manufacturer's standard.

6.Transmissivity or Flow Q of composite construction, geotextile bonded to core 					when tested in accord with ASTM D-4716-01 with hydraulic gradient of .1 with 					confining stress of 3600 PSF: 30.0 gallons/min/ft (372 lpm/m)

7.Furnish manufacturer's 12"x12" corner fittings and 12"x 4" end outlet, 12"x 4" 		 			side outlet and 12" x 4" corner outlet fittings with 4" diameter female connector 					for  connection to 4" diameter corrugated plastic piping system specified 					elsewhere.

Specifier Note: Use furring strips if Method 2 installation indicated on drawings for vertical installation

E. Furring Strips: Pressure treated lumber specified in Rough Carpentry Section

PART 3-EXECUTION

3.01 	EXAMINATION

A.	Verification of Conditions

**1.	Verify waterproofing protection material is in place if specified in section 0700

2.	Examine site conditions and substrates where products specified in this section 					are to be installed.  Submit written notification if conditions are unacceptable.

3.02 INSTALLATION

Specifier Note: Foundation vertical wall installation hangs material vertically full depth in one pass lapping filter material at vertical joist.  Method requires full height backfill after all material is installed.  Vertical installation can be done in lifts if desired.

Specifier Note: Horizontal installation runs material horizontally allowing separate lifts in backfill.  Can leave selection to the contractor if there are no special requirements.

Specifier Note: Foundation wall method 1 utilizes adhesive application at drainage material top. Method 2 utilizes wood furring strip to hold material at finish grade level in place until backfilled.

Specifier Note: Horizontal application with vehicular traffic is not recommended.

A.	Foundation Wall Installation

1.	Install subdrainage system material **either** vertically or **horizontally** in accord 						with manufacturer's reviewed installation instructions with core material facing 						protection board or waterproofing.

2.	Lap geotextile fabric joints in accord with manufacturer's installation instructions.

**3.	Tie subdrainage material into previously installed vertical collection system material 						in accord with subdrainage system manufacturer's reviewed details for positive 						drainage directly to vertical collection system.

Specifier Note: Use above in connection with vertical collection system indicated below.  Use below if only perforated drainage piping used and specified in another section

**4.	Install subdrainage material at foundation drainage pipe material in accord with 						subdrainage system manufacturer's reviewed details for positive drainage directly to 					foundation drainage pipe.

**5.	Horizontal Application: Verify backfill lifts are installed and compacted prior to 							installation of next subdrainage system material course.

**6.	Secure subdrainage system material to wall at grade in accord with manufacturer's 							indicated and reviewed installation instructions.

B. LAGGING INSTALLATION

1.	Install subdrainage system material vertically in accord with manufacturer's reviewed 					and installation instructions.

2.	Lap geotextile fabric joints in accord with manufacturer's installation instructions.

**3.	Tie subdrainage material into previously installed vertical collection system material 							in accord with subdrainage system manufacturer's reviewed installation details for 						positive drainage directly to vertical installation system.

Specifier Note: Use above in connection with vertical collection system indicated below. Use below if only perforated drainage piping used and specified in another section.

**4.	Install subdrainage material at foundation drainage pipe material in accord with 							subdrainage system manufacturer's reviewed details for positive drainage directly to 						foundation drainage pipe.

5.	Secure subdrainage system material to wall at grade in accord with manufacturer's 							indicated and reviewed Method 2, wood strip.

C. Modular Chimney drainage system installation

1.	Unroll material horizontally along foundation base, adhere to partially cured 							waterproofing or fasten with powder activated mechanical fastener.  Application to 							sheet waterproofing use adhesive accepted by waterproofing manufacturer or 							powder activated mechanical fastener.

2.	Install preformed corner fittings  at foundation interior and exterior corners.

3	Install outlet fittings where indicated; connect to corrugated drainage pip if present at 						the time of installation; leave ready for connection to corrugated pipe if not present at 						time of installation.

4.	Install vertical chimney sections in accord with manufacturer's installation 								instructions; tie into continuous horizontal footing drain.  Vertical chimneys wll be 							spaced 4'-6' on center.  Adhere to waterproofing with acceptable adhesive or 							powdered activated mechanical fastener.

D. Vertical collection system

1.	Unroll material along foundation base; adhere to partially cured waterproofing 							material; use adhesive acceptable to waterproofing manufacturer for cured 							waterproofing or sheet waterproofing.  Or adhere with powder activated mechanical 							fasteners.

2.	Install preformed corner fittings at foundation interior and exterior corners.

3	Install outlet fittings where indicated; connect to corrugated drainage pip if present at 						the time of installation; leave ready for connection to corrugated pipe if not present at 						time of installation.

4.	Cover remainder of wall other DrainGuard Wall Drainage Systems

# Text boxes

| Specifier Note: |
| --- |
| Product Selection Guide |
| Application | Product |
| Foundation Walls | DrainGuard 400/420 |
| Retaining Walls | DrainGuard 400/420 |
| Lagging Walls | DrainGuard 400/420 |
| Underslab (ongrade) | DrainGuard 400 |
| Crib Walls | DrainGuard 400 |
| Retaining/Foundation Walls | Modular Drainage System |
| Trench Drains | DrainGuard 6" or 12" |
| Edge Drains | DrainGuard 6" or 12" |
| Split Slab (non vehicular traffic) | DrainGuard 700/720 |
| Planters | DrainGuard 700/720 |
| Plaza Decks (non vehicular traffic) | DrainGuard 700/720 |